Mass balance zeolite columns

Raw water during first cycle (virgin zeolites)

Average NH4+-concentration: 5.85 mg/l

Total runtime: 2610 min = 43,5 h

L columns = 110 cm (V=0.885 l)

Estimated porosity = 40 %

Pore volume = 0.35 l

NaOH concentration 0.1 mol/l

5 flushes = 1.75 l NaOH per column (0.175 mol NaOH)

7 flushes = 2.45 l NaOH per column (0.245 mol NaOH)

Column 1 (Clinoptilolite w/ NaOH)

Flowrate: 3.43 l/h

Total ammonium entered: 3.43*43.5*5.85 = 872.85 mg => 0.87 g

Total ammonium in effluent:

99.3 mg (surface area underneath effluent graph)

Removed by zeolites:

872,85 – 99.3 = 773.55 mg (=0.043 mol)

Column 2 (Aqualite w/ NaOH)

Flowrate: 3.64 l/h

Total ammonium entered: 3.64*43.5*5.85 = 926.29 mg

Total ammonium in effluent:

67.3 mg

Removed by zeolites:

926.29 – 67.3 = 858,97 mg (= 0.048 mol)

Colum 3 (Clinoptilolite w/ NaCl-NaOH)

Flowrate: 3.52 l/h

Total ammonium entered: 3.52*43.5*5.85 = 895.75 mg

Total ammonium in effluent:

102.93 mg

Removed by zeolite:

895.75 – 102.93 = 792.82 mg (= 0.044 mol)

Column 4 (Aqualite w/ NaCl-NaOH)

Flowrate: 3.93 l/h

Total ammonium entered: 3.93*43.5*5.85 = 1000.13 mg

Total ammonium in effluent:

100.44 mg

Removed by zeolite:

899.69 mg (=0.050 mol)