# Appendix B	Sieve Curves

The procedure for the selection of the stones with a certain dn50 is given in the following steps.

The first four steps are the same all stone sizes:

Step 1		Sieve the stones using two sieves, one with gaps a little larger than the other.

Step 2		Wash the collected stones carefully.

Step 3	Dry the stones.

Step 4		Collect a random large amount of stones from the sieved washed and dried stones. (≥ 144)

Step 5		Weigh each stone separately using an accurate balance. Weigh each stone dry and under water and register the values.

Step 6	Measure the largest length and the smallest length of each stone using an accurate ruler.

Step 7		Make the following calculations for determining the stone parameters:

ρs=ρwMdrMw							(3.7)

Vs=1ρsMdr						(3.8)

dn=3Vs							(3.9)

All the necessary stone parameters can now be calculated.

Dessens (2004) performed the procedures for determining the stones parameters with the following dn50 = 0.0082m and dn50 = 0.0200m

In figure B.1 is a distribution of the dry mass is plotted versus the percentage of the cumulative weight for the smaller grain size. Also a distribution of the diameter of the grains (dn) is plotted versus the cumulative weight is given in figure B.2. For the sieve curves of the larger grain size see The influence of flow acceleration on stone stability (Dessens, 2004)

For the determination of the stone parameters of the small stones 250 grains were measured.

Table B.1  contains the important parameters for these stones.

Table B.1	Stone parameters (Dessens, 2004)

|  | Small stones | Large stones | Dimension |
| --- | --- | --- | --- |
| # stones | 250 | 139 | - |
| M cum. | 361.77 | 2845.6 | gr |
| dn50 | 0.0082 | 0.0200 | m |
| ρ av. | 2682.2 | 2682. | kg/m3 |
| W50 | 1.49 | 21.422 | gr |
| d85/d15 | 1.22 | 1.18 | - |
| Δ | 1.67 | 1.67 | - |

Now the sieve curves are presented in figure B.1 and figure B.2

Figure B.1	Mass distribution small stones, dn50 = 0.0082m

Figure B.1	Dn distribution small stones, dn50 = 0.0082m