# Effect of Compression

To determine the following aspects:

Effects of compression time and force. It is now evident that correct formation of initial contact forms the base of the adhesion properties. Therefore, several experiments are conducted :

| Test: | Compression Force | Compression Time | Amount of samples |
| --- | --- | --- | --- |
| 1 | 1 | 10 | 3 |
| 2 | 1 | 30 | 3 |
| 3 | 1 | 60 | 3 |
| 4 | 5 | 10 | 3 |
| 5 | 5 | 30 | 3 |
| 6 | 5 | 60 | 3 |
| 7 | 10 | 10 | 3 |
| 8 | 10 | 30 | 3 |
| 9 | 10 | 60 | 3 |

Constant parameters are:

| Parameter |  |  |
| --- | --- | --- |
| Temperature | 340 | C |
| Compression Force | - | N |
| Compression Time | - | sec |
| Compression sample rate | 1 | Hz |
| Displacement rate | 0.05 | mm sec-1 |
| Displacement sample rate | 200 | Hz |
| Relaxation Time | 10 | Sec |

## Test 1:

Date: 20220906

Analyse these tests with ‘Adhesion_CompressionEffect.m’

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc10_1_1 tm 4 | 20220901- 10 (CoConsolidated) | 20220901 -29 (CoConsolidated) |

Fc1Tc10_1_1 was not carried out correctly. The rheometer controller was not quick enough to reach the 1N setpoint within 10 seconds. Therefore, for tests 2,3 & 4, compression time was set to 20 sec. This meant the actual compression time did take 10 seconds.

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc10_2_1 tm 3 | 20220901 - 47 (CoConsolidated) | 20220901 -56 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc10_3_1 tm 3 | 20220901 - 55 (CoConsolidated) | 20220901 -33 (CoConsolidated) |

## Test 2:

Date: 20220906

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc30_1_1 tm 3 | 20220901- 35 (CoConsolidated) | 20220901 -40 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc30_2_1 tm 3 | 20220901 - 14 (CoConsolidated) | 20220901 -24 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc30_3_1 tm 3 | 20220905 - 56 (CoConsolidated) | 20220905 -40 (CoConsolidated) |

## Test 3:

Date: 20220906

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc60_1_1 tm 3 | 20220905- 10 (CoConsolidated) | 20220905 - 55 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc60_2_1 tm 3 | 20220905 – 41 (CoConsolidated) | 20220905 - 47 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc1Tc60_3_1 tm 3 | 20220905 - 25 (CoConsolidated) | 20220905 - 64 (CoConsolidated) |

## Test 4:

Date: 20220908

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc10_1_1 tm 3 | 20220905- 60 (CoConsolidated) | 20220905 – 42 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc10_2_1 tm 3 | 20220905 – 54 (CoConsolidated) | 20220905 - 33 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc10_3_1 tm 3 | 20220905 - 62 (CoConsolidated) | 20220905 - 12 (CoConsolidated) |

## Test 5:

Date: 20220908

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc30_1_1 tm 3 | 20220907 -20 (CoConsolidated) | 20220907 – 54 (CoConsolidated) |

Temperature dropped during 2nd test to approximately 333 degrees C

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc30_2_1 tm 3 | 20220907 – 13 (CoConsolidated) | 20220907 – 37 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc30_3_1 tm 3 | 20220907 - 28 (CoConsolidated) | 20220907 - 4 (CoConsolidated) |

## Test 6:

Date: 20220908

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc60_1_1 tm 3 | 20220907- 53 (CoConsolidated) | 20220907 – 63 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc60_2_1 tm 3 | 20220907 – 17 (CoConsolidated) | 20220907 - 46 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc60_3_1 tm 3 | 20220907 - 21 (CoConsolidated) | 20220907 - 38 (CoConsolidated) |

## Test 7:

Date: 20220909

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc10_1_1 tm 3 | 20220907- 59 (CoConsolidated) | 20220907 – 30 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc10_2_1 tm 3 | 20220907 – 48 (CoConsolidated) | 20220907 - 9 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc10_3_1 tm 3 | 20220907 - 2 (CoConsolidated) | 20220907 -19 (CoConsolidated) |

## Test 8:

Date: 20220909

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc30_1_1 tm 3 | 20220907- 61 (CoConsolidated) | 20220907 – 29 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc30_2_1 tm 3 | 20220907 – 43 (CoConsolidated) | 20220907 - 22 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc30_3_1 tm 3 | 20220907 - 3 (CoConsolidated) | 20220907 -6 (CoConsolidated) |

## Test 9:

Date: 20220909

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc60_1_1 tm 3 | 20220907- 27 (CoConsolidated) | 20220907 – 26 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc60_2_1 tm 3 | 20220907 – 39 (CoConsolidated) | 20220907 - 11 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc10Tc60_3_1 tm 3 | 20220907 - 44 (CoConsolidated) | 20220907 -45 (CoConsolidated) |

## Test 10:

Date: 20220927

Tests 10 and 11 were later carried out with 5N of compression force and higher compression times (240 and 480 sec).

NOTE: Analyze these tests with  ‘Adhesion_CompressionEffect_v2’!!

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc240_1_1 tm 3 | 20220926 - 10 (CoConsolidated) | 20220926 - 21 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc240_2_1 tm 3 | 20220926 - 16 (CoConsolidated) | 20220926 - 20 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc240_3_1 tm 3 | 20220926 - 13 (CoConsolidated) | 20220926 - 19 (CoConsolidated) |

## Test 11:

Date: 20220927

Tests 10 and 11 were later carried out with 5N of compression force and higher compression times (240 and 480 sec).

| Set 1: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc480_1_1 tm 3 | 20220926 - 17 (CoConsolidated) | 20220926 - 25 (CoConsolidated) |

| Set 2: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc480_2_1 tm 3 | 20220926 - 27 (CoConsolidated) | 20220926 - 22 (CoConsolidated) |

| Set 3: | Specimen on top | Specimen on bottom |
| --- | --- | --- |
| Fc5Tc480_3_1 tm 3 | 20220926 – 12 (CoConsolidated) | 20220926 - 24 (CoConsolidated) |