## Slide 1: Fitting of Hex-Ge spectra

## Slide 2: Model 3: Lasher-Stern-Wurfel model
Fitting Parameters: A, Eg, Telectron,γ ,d ,Δμ
In this equation is the splitting of the quasi-fermi levels and is the absorptivity instead of the absorption coefficient, this is to correct for reflections from the surface and reabsorption given by:
In which is a characteristic absorption length but I just absorb it into the absorption coefficient which has a fitting parameter A explained on the next slide.
This model was originally written down by Würfel who investigated how black-body-radiation and radiation of a two-level system are related by introducing a chemical potential.
Reference:
Slight modifications were made by Lasher and Stern who corrected the absorption coefficient for re-absorption processes.

## Slide 3
In the first approximation the absorption coefficient is proportional to the density of states and the density of states is given by a square root function . To also take into account states in the bandgap (due to doping) the density of states is convoluted with a peak function T(E). Which gives an absorption coeff G(E).
Model 3: Lasher-Stern-Wurfel model
The formula for T(E) is a generalised form in which gives the “sharpness”of the peak as is typically chosen to be in between 1 and 2, is a fitting parameter determining the width of the peak and N is a normalization constant that makes sure the integral under the peak remains 1. Examples of the peaks with are plotted on the right together with the corresponding G(E) funtions

## Slide 4: Model 3: Lasher-Stern-Wurfel model
The problem of this model is that it has a singularity when . This can be understood because we assume the absorption coefficient to be independent of the occupation by charge carriers, however if fermi-levels are inside the band some transitions become inaccessible. And example of such a singularity is show in blue in the figure which is not corrected and red which is the occupation corrected PL spectrum. .
Correcting the absorption coefficient for occupation gives:
When assuming intrinsic.
This derivation can be found in reference:

## Slide 5: Model 3: Lasher-Stern-Wurfel model
T-series
Fitting Parameters: A, Eg, Telectron,γ ,Δμ

## Slide 6: Model 3: Lasher-Stern-Wurfel model
T-series
Fitting Parameters: A, Eg, Telectron,γ ,Δμ

## Slide 7: Model 3: Lasher-Stern-Wurfel model
P-series
Fitting Parameters: A, Eg, Telectron,γ ,Δμ

## Slide 8: Model 3: Lasher-Stern-Wurfel model
P-series
Fitting Parameters: A, Eg, Telectron,γ ,Δμ

## Slide 9: Model 3: Lasher-Stern-Wurfel model
Future improvements:
Correct for the inhomogeneous occupation of valence and conduction band due to doping
Correct for a small absorption contribution at 0.35 eV
Try to estimate the free carrier density
Try to determine the doping level in the Ge-shell using this model
Make a fit using density of states data from Jena (prefearably a DOS per transition such that the exact energies can still be fitted )
Measure a power series at higher excitation density to see whether the second peak can be included in the model
Measure a temperature series at lower excitation density to see how the charge carriers relax
Measure a RT power series to see if we can go down to the temperature effects driven by the lattice.